## Slide 1
GDR Prométhée Scientific Days
Hydrometallurgical recovery of tin and copper from mobile phone printed circuit boards.
L’Hôte Marianne1, Meux Eric1, Leclerc Nathalie1, Philippe Pierrat2, Hervé Muhr3, Yosri Khalsi4, Frédéric Diot5
Thursday June 5th 2025, ISEA Metz
1 Institut Jean Lamour, Metz
2 Laboratoire Lorrain de Chimie Moléculaire, Metz
3 Laboratoire Réactions et Génie des Procédés, Nancy
4 CRITT-Techniques Jet Fluide et Usinage, Bar-le-Duc
5 GeoRessources, Vandœuvre-lès-Nancy

## Slide 2: Introduction
THYMO Project (HYdrometallurgical Treatment of MObile phones)
Over 120 millions mobile phone remain in French drawers !
Flows and fleets of mobile phones in France in 2018. [1]
[1] Sofies and Bio Innovation Service (2019). Étude du marché et parc de téléphones portables français en vue d’augmenter durablement leur taux de collecte.
Notes: Mise sur le marché

## Slide 3: THYMO Goals
Develop an innovative process for recycling cell phone circuit boards:
low environmental impact
energy-efficient
enables maximum recovery of metals
enables the “polymer” part of the board to be recovered
Use a significant quantity of circuit boards to obtain realistic raw material
Collection of over 19000 mobiles phones

## Slide 4: Phone disassembly
Printed circuit boards or PCBs
Theoretical industrial rate : up to 400 phones per minute
Automated process by CRITT-TJFU
Notes: Centre de recherche
Reactif eau abrasif, et sera recyclée

## Slide 5: PCBs Shredding
Magnetic sorting
Eddy Current
Shredding (hammer mill)
PCBs from
CRITT TJFU
Shredding to 8 mm
Sizing < 500 µm
Shaking table
Heavy fraction : metals, ceramics (BaSO4, Al2O3)
Light fraction : epoxy resin, glass fibers, aluminum
Pre-treatment
Notes: Photo table secousses

## Slide 6: Characterization
Shredded PCBs
Pmax = 1,8 kW T° = 220 °C t = 20 mn
3 replicates
Homogenization
Aqua regia leaching
20 mL HNO3/HCl
Filtering 0,45 µm
ICP-AES
Leachate
Solid residues
XRD, CHNS
500 mg
Elementary analysis
200 g
Characterization protocol
Notes: Ne pas dire « plus en détails » Rajouter concentration eau régale
Dire que mon travail ici

## Slide 7: Characterization
PCB shred composition
Metals | Weight fraction (%)
Cu | 52-70
Sn | 7-15
Ni | 2-4
Al | 0.2-1.2
Fe | 0.9-1.8
Zn | 0.2-1.6
Pb | 0.1-1
Ag | 0.03-0.2
Au | 0.1-0.15
Pd | < 0.05
90 % of market value
Notes: AGGRANDIR

## Slide 8: Process overview
Leaching H2O2 / H2SO4
Shreds ( < 500 µm)
L/S separation
SnO2, xH2O precipitation
Removal of Al3+ and Fe3+
Residues (Ag2SO4, PbSO4, Au, Pd…)
Leachate (Cu2+, Sn4+, Ni2+, Zn2+, Al3+, Fe3+)
Ni2+ and Zn2+ solution
Copper electrolysis
NaOH
Phytic acid
Metallic copper
Metallic phytates
Stannic acid
Notes: On ne « créer » pas de phytates
Dire élimination é
Dire précipitation phyate
ventuelles si concen

## Slide 9
Leaching step

## Slide 10: Leaching step (1/3)
Reagents
H2O2-H2SO4 (H2O2 considered as a green oxidant)
Cu(s) + H2O2 (aq) + 2 H+(aq) → Cu2+(aq) + 2 H2O(l)
Sn(s) + 2 H2O2 (aq) + 4 H+ (aq) → Sn4+ (aq) + 4 H2O(l)
Constraints
Limit H2O2 dismutation (temperature, catalysis by Cu2+, Fe2+, Fe3+)
Avoid CuSO4, 5H2O precipitation (solubility of 207 g/L in water at 20°C)
Avoid prematured precipitation of SnO2, x H2O

## Slide 11: Leaching step (2/3)
Optimal conditions
n H2O2 / Σ n métaux = 2
n H+ / Σ n métaux = 6
Leaching time = 4h
Liquid/Solid ratio = 14 mL/g
Cryostat set at 20°C
Stirring rate = 300 rpm
Tested on 3 leachings
Copper leaching rate : 82.8 ± 4.4 %
Tin leaching rate: 96.1 ± 0.5 %
Optimization – Design of Experiments
Fractional factorial design 24-1 then central composite design
L/S = 14 mL/g
Notes: Formule sigma pour stoechio
Rapport molaire
Augmenter police graph
Mettre flèche avec augm temps et H2O2
Rajouter cercke
Enlever « copper leaching eate » au dessus des couleurs

## Slide 12: Leaching step (3/3)
Optimization – Multi-step leaching
H2O2 quantity divided between 2 leaching steps
Second leaching on residues from the previous one
3 protocols were studied
1-step leaching with 100 % H2O2
2-steps leaching 50-50 % H2O2
2-steps leaching 75-25 % H2O2
Leaching protocol | One step: 100% H2O2 | 1st step: 50% H2O2 2nd step: 50% H2O2 | 1st step: 75% H2O2 2nd step: 25% H2O2
Final copper leaching rate (%) | 82.8 ± 4.4 | 97.3 ± 1.1 | 95.9 ± 2.2
Final tin leaching rate (%) | 96.2 ± 0.5 | 97.8 ± 0.2 | 97.6 ± 0.3
Notes: Séparer ou fractionner en deux

## Slide 13
Recovery of tin

## Slide 14: Recovery of tin (1/2)
Leaching H2O2 / H2SO4
S/L separation
SnO2, x H2O precipitation
Leachate (Cu2+, Sn4+, Ni2+, Al3+, Fe3+, Zn2+)
NaOH
Stannic acid
Problems :
Spontaneous precipitation of stannic acid at pH ≃ 0.3 – 0.5
Important increase of pH → may decrease purity (goethite precipitation, Cu2+ adsorption)
Crystal seeding at lower pH → requires pre-made stannic acid
Goal : Precipitate stannic acid selectively and quantitatively
Precipitation delay
Notes: AGGRANDIR

## Slide 15: Recovery of tin (2/2)
Initial leachate [H+] > 1 mol/L
Leachate pH = 0
Leachate pH = 1
NaOH 5-6 mol/L
Pur germs (50 g/L solution)
NaOH 5-6 mol/L
Centrifugation + filtering
Leachate
[Cu2+] = 3.76.10-1 mol/L or 24 g/L
[Sn4+] = 6.57.10-5 mol/L or 8 mg/L
%Cu trapped = 2.4%
Washing by repulping: 1 mL H2SO4 0,1 M per gram of precipitate
[Cu2+] = 1.72.10-1 mol/L
%Cu trapped = 1,8 %
[Cu2+] = 7.96.10-2 mol/L
%Cu trapped = 1.4 %
[Cu2+] = 4.94.10-2 mol/L
%Cu trapped = 1.1 %
Washing 1
Washing 2
Washing 3
Crystal seeding

## Slide 16
Scale-up
Notes: Changement d’échelle
5g à +100g

## Slide 17: Scale-up (1/3)
Leaching step
Two-step leaching in optimal conditions in a 3 L reactor
Leachates gathered into one
Metals | Concentration (g/L) | Concentration (mol/L) | Leaching rate (%)
Cu | 37.93 | 5.97*10-1 | > 95
Sn | 5.63 | 4.8*10-2 | > 95
Ni | 0.83 | 1.4*10-2 | 
Zn | 0.49 | 7.5*10-3 | 
Fe | 0.17 | 3.0*10-3 | 
Al | 0.02 | 7.4*10-4 | 
Optimal conditions
n H2O2 / Σ n métaux = 2 (50-50) n H+ / Σ n métaux = 6
Leaching time = 4 h Liquid/Solid ratio = 14 mL/g
Cryostat set at 20°C Stirring rate = 300 rpm
140 g of shreds
Notes: Changement d’échelle 5g à 140g
Mettre taux lixi cu et sn en rouge

## Slide 18: Scale-up (2/3)
Leaching step
Mass loss ≃ 82%
BEFORE
AFTER
Metals | Cu | Sn | Ni | Zn | Fe
Mass content (%) | 69.3 | 12.2 | 2.6 | 1.6 | 0.9
Metals | Al | Pb | Ag | Au | Pd
Mass content (%) | 0.2 | 0.9 | 0.2 | 0.09 | 0.05
Metals | Cu | Sn | Ni | Zn | Fe
Mass content (%) | 21.2 | 2.6 | 6.4 | 0.6 | 5.5
Metals | Al | Pb | Ag | Au | Pd
Mass content (%) | 0.6 | 5.7 | 1.1 | 0.26 | 0.17
Notes: Mettre échelle

## Slide 19: Scale-up (3/3)
Tin recovery
Best results at pH = 2.5
Metals | Concentration (g/L) | Concentration (mol/L)
Cu | 23.21 | 3.65*10-1
Sn | 0.10 | 8.4*10-4
Ni | 0.46 | 7.8*10-3
Zn | 0.29 | 4.4*10-3
Fe | 0.10 | 1.8*10-3
Al | < 0.01 | < 3.7*10-4
After 1 wash : 1% copper remaining in precipitate
Low amount of aluminum and iron
-> phytates precipitation step is skipped
Next steps :
Copper electrolysis
Recovery of nickel and zinc (chelating resin)
Notes: Revoir cadre vert

## Slide 20: Conclusion
Savings in H2O2 consumption with two-step leaching process
Production of a tin precipitate richer than cassiterite
  SnO2, 2 H2O (around 1% Cu trapped) represents around 70 % SnO2
   production of tin via pyrometallurgy or electrolysis in alkaline medium
Maximization of both copper and tin leaching from PCB shreds (< 500 µm) by Design of Experiments methodology
Leaching rates of copper and tin > 97 %
Notes: 3) Recup étain sosu forme sno2 2H20 (+riche que cassi) -> produc pyro
A VERUFUER EN JAUNE
Perspectives

## Slide 21: Prospects
Electrolysis of copper incoming
  - Purity of at least 99,99 % required
  - Avoid co-deposition of nickel
Mineralurgical characterization of leaching residues (at least 100 g required)
Development of precious metals enrichment process according to density, electrical conductivity, magnetic susceptibility of different phases
Notes: À l »oral : recup du cuivre par eelec